LIQUID DAMPPROOFING & WATERPROOFERS

|  |  |  | COMPARISON CHART |
| --- | --- | --- | --- |
|  | M A S C O . N E T |  |  |

| LIQUID DAMPROOFERS & WATERPROOFERS |  |  | COVERAGE | CONDITION | CONCRETE | PARGED BLOCK |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | SIZE | # |  | 1ST | 2ND | DAMP | AGE | EXT | CAVITY | EXT | CAVITY | INITIAL | FULL | APPLICATION |
| CODE | PRODUCT |  | DESCRIPTION | UNIT | APP |  | SF/GAL | SF/GAL | SURF | CONC | BELOW | ABOVE | BELOW | ABOVE | CURE | CURE | TROWEL | BRUSH | ROLL |
| DAMPROOFING | EMULSION |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| TAM 5G75 | DEHYDRATINE 75 |  | NON FIBERED ROLL GRADE | 5 GAL | 2 |  | 50 | 50 | YES | 2 DAY | YES | YES | YES | YES | 24 HR | 48 HR | NO | YES | YES |
| TAM 5G85 | DEHYDRATINE 85 |  | FIBERED BRUSH GRADE | 5 GAL | 2 |  | 50 | 50 | YES | 2 DAY | YES | YES | YES | YES | 24 HR | 48 HR | NO | YES | YES |
| TAM 5G95 | DEHYDRATINE 95 |  | FIBERED TROWEL GRADE | 5 GAL | 2 |  | 50 | 50 | YES | 2 DAY | YES | YES | YES | YES | 24 HR | 48 HR | YES | NO | NO |
| DAMPROOFING | SOLVENT |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| TAM 5G4 | DEHYDRATINE 4 |  | NON FIBERED ROLL GRADE | 5 GAL | 2 |  | 75 | 125 | NO | 28 DAY | YES | NO | YES | NO | 24 HR | 48 HR | NO | YES | YES |
| TAM 5G6 | DEHYDRATINE 6 |  | FIBERED TROWEL GRADE | 5 GAL | 2 |  | 50 | 50 | NO | 28 DAY | YES | NO | YES | NO | 24 HR | 48 HR | YES | NO | NO |
| WATERPROOFING ELASTOMERIC |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| AC 5GSRG | STRATASEAL RG |  | ROLLER GRADE | 5 GAL | 2 |  | 40 | 40 | YES | 7 DAY | YES | YES | YES | YES | 24 HR | 48 HR | NO | YES | YES |
| AC 5GSTG | STRATASEAL TG |  | TROWEL GRADE | 5 GAL | 2 |  | 40 | 40 | YES | 7 DAY | YES | YES | YES | YES | 24 HR | 48 HR | YES | YES | NO |

APPLICATIONS:

DAMPROOFING STEM WALLS

WATERPROOFING BELOW GRADE BASEMENTS

CAVITY WALL DAMPROOFING

WATERPROOFING CONCRETE DECKS

THIS CHART SHOULD BE CONSIDERED A GUIDE ONLY

CONSULT SPECIFICATIONS SHEETS FOR COMPLETE TECHNICAL,

INSTALLATION AND SURFACE PREP PROCEDURES

ALL TESTING PERFORMED @ 72 F

APPLICATION TEMPERATURE BETWEEN 40-90 F

| FOUNDATION DRAINAGE BOARDS |  |  |  |  |  | PROPERTIES |  |  | APPLICATION SURFACES |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | ROLL |  | QTY | THICK | FLOW | PSI | MAX | BELOW GRADE | SPLIT | PARGED |  |  | CONFINE |
| CODE | PRODUCT | DESCRIPTION | SIZE | SF | LBS | PLT | NESS | RATE | RATING | DEPTH | VERT | ROOF |  | SLAB | SLAB | BLOCK |  | CONC | MENT |
| DRB 2000 | DELTA DRAIN 2000 | NON WOVEN FABRIC | 4' X50' | 200 | 38 | 6 | .4" | 18 GL | 11,000 | 16' | YES | YES |  | NO | NO | YES |  | YES | YES |
| DRB 6000 | DELTA DRAIN 4000 | NON WOVEN FABRIC | 4' X50' | 200 | 42 | 6 | .4" | 18 GL | 15,000 | - | YES | YES |  | NO | NO | YES |  | YES | YES |

APPLICATIONS:	THIS CHART SHOULD BE CONSIDERED A GUIDE ONLY

FOUNDATION DRAINAGE BOARD	CONSULT SPECIFICATIONS SHEETS FOR COMPLETE TECHNICAL,

PROTECTION COURSE FOR WATERPROOFING	INSTALLATION AND SURFACE PREP PROCEDURES